|  | VKS TECH Met Operational Excellence | Doc: VKS/MET/SOP/04 Rev: 01 April 2026 |
| --- | --- | --- |
|  | Standard Operating Parameters — AlBond Metallization | Scope: Met-1 & Met-2 |
|  | vkstech.com ¦ Free Industrial Knowledge for Packaging Professionals |  |

🎯 Purpose

Maintaining quality of Metal Bond Strength (AlBond) in metallised finished rolls through controlled process parameters.

📊 AlBond Material — Type ABM (Oxygen-Enhanced)

Base Film Type: G301 series (PET). Optical Density: 2.2 to 2.5

| Parameter | Value | Unit |
| --- | --- | --- |
| AlBond Intensity (O₂ Supply) | 5.0 to 5.5 | Machine Recipe (~400 SCCM) |
| Speed of Machine | 650 | Metre/Min |
| Plasma Unit Power | 5 | kW |
| Plasma Unit Gas Flow | 1000 | SCCM |
| Oxygen Gas Supply | 80 | % |

⚠️ Above are MAXIMUM values. Base film must have surface energy greater than 54 Dynes for proper bond strength.

📊 Standard Met Material — Type M (No Oxygen)

Base Film Type: G301 series (PET). Optical Density: 2.2 to 2.5

| Parameter | Value | Unit |
| --- | --- | --- |
| AlBond Intensity (O₂ Supply) | 4.0 to 4.5 | Machine Recipe (~320 SCCM) |
| Speed of Machine | 750 | Metre/Min |
| Plasma Unit Power | 5 | kW |
| Plasma Unit Gas Flow | 1000 | SCCM |
| Oxygen Gas Supply | 80 | % |

⚠️ Surface energy must be greater than 54 Dynes for both material types.