|  | VKS TECH Met Operational Excellence | Doc: VKS/MET/SOP/05 Rev: 01 April 2026 |
| --- | --- | --- |
|  | Standard Operating Parameters — CPP Metallization | Scope: Met-1 & Met-2 |
|  | vkstech.com ¦ Free Industrial Knowledge for Packaging Professionals |  |

🎯 Purpose

Maintaining quality of CPP Metallised Film with controlled waste: 5.1% (4.1% Sheet 600M/14500M, 1% Trim 20mm/2000mm).

📋 Material Type

30 MIC CPP, 20 MIC CPP (COF: 0.2). Average Width: 2090 mm. Jumbo Length: 14,500 Metres. Target OD: 2.2

📊 Standard Operating Parameters

| S.No. | Parameter | Value | Unit |
| --- | --- | --- | --- |
| 1 | Coating Drum Temperature | -20 | Degree Celsius |
| 2 | Speed of Machine | 660 | Metre/Min |
| 3 | Rewinder Tension (2090mm) | 120 to 150 | Newton |
| 4 | Rewinder Winding Direction | OUT | Threading Direction |

⚠️ COF 0.2 + Anti-Blocking Agent requires Tension 120-150N. Winding direction must ALWAYS be OUT.