|  | VKS TECH Met Operational Excellence | Doc: VKS-MET-SOP-06 Rev: 01 April 2026 |
| --- | --- | --- |
|  | OD Set Parameters | Scope: Metalliser-1 & 2 |
|  | vkstech.com ¦ Free Industrial Knowledge for Packaging Professionals |  |

🎯 Purpose

1. Bare Waste Percentage should not exceed 500 metres (1%) in one Jumbo.

2. Optical Density values of material should be produced within specified range strictly.

📊 OD Set Point Table — Customer-wise Targets

Inline OD Sensor (Hawkeye) set points for standard metallization:

| Customer OD | Min (-5%) | Max (+5%) | Met-1 Max | Met-2 Max | Special Max |
| --- | --- | --- | --- | --- | --- |
| 2.2 | 2.09 | 2.31 | 2.2 | 2.2 | 2.4 |
| 2.5 | 2.37 | 2.63 | 2.5 | 2.5 | 2.7 |
| 2.8 | 2.66 | 2.94 | 2.8 | 2.8 | 3.0 |

👤 Responsibility

Met Operators: Maintain OD set points as per table above on the inline sensor system.

Supervisor: Ensure quality of material and OD is produced as per set points to maintain Aluminium wire consumption under control.

⚠️ Supervisor must verify OD set points match customer requirement before every new jumbo. Over-coating wastes aluminium wire; under-coating causes barrier failure.