|  | VKS TECH Met Operational Excellence | Doc: VKS/MET/SOP/07 Rev: 01 April 2026 |
| --- | --- | --- |
|  | Bare Waste Control — Unwinder Stop Diameter | Scope: Met-1 & Met-2 |
|  | vkstech.com ¦ Free Industrial Knowledge for Packaging Professionals |  |

🎯 Purpose

1. Bare Waste Percentage should not exceed 500 metres (1%) in one Jumbo.

2. Optical Density values must be produced within specified range strictly.

📊 Unwinder Stop Diameter Set Points

Met-1 Settings

| Core Type | Core Size | Stop Diameter (mm) |
| --- | --- | --- |
| Steel Core | 6 inch | 181 |
| Paper Core (12mm wall) | 6 inch | 184 |
| Paper Core (14mm wall) | 6 inch | 188 |

Met-2 Settings

| Core Type | Core Size | Stop Diameter (mm) |
| --- | --- | --- |
| Steel Core | 8 inch | 222 |
| Paper Core (17mm wall) | 8 inch | 241 |
| Paper Core (19mm wall) | 8 inch | 245 |

👤 Responsibility

Met Operators: Maintain stop diameter set points as per table above.

Supervisor: Ensure bare waste is less than 500 metres per jumbo. Target: 0.7%.

⚠️ Running below stop diameter risks core damage and excessive bare waste. Always verify set point before starting a new jumbo.