|  | VKS TECH Met Operational Excellence | Doc: VKS/MET/SOP/09 Rev: 01 April 2026 |
| --- | --- | --- |
|  | Slitting Parameters for Ripple-Free Material | Scope: Met Slitter-1 & 2 |
|  | vkstech.com ¦ Free Industrial Knowledge for Packaging Professionals |  |

🎯 Purpose

To produce material that is Ripple and Vertical Line Impression Free.

📊 Standard Operating Parameters

| Parameter | Set Point |
| --- | --- |
| Rewinding Tension | 90 N/M |
| Rewinding Nip Pressure | 700 N/m² |
| Speed | 500 M/Min |
| Unwinder Tension | 90 N/M |

👤 Responsibility

Slitter Operators: Ensure nip roll being used does not have any non-uniformity or cut marks on its surface. Maintain set point values as per above standards.

Supervisor: Ensure quality of material is ripple-free and does not have any vertical line impression on finished roll.

⚠️ If nip roller has any surface defect, replace BEFORE running. Damaged nip = guaranteed ripple marks on every roll.