|  | VKS TECH Met Operational Excellence | Doc: VKS/MET/SOP/12 Rev: 01 April 2026 |
| --- | --- | --- |
|  | Slitting Parameters for Scratch-Free Material | Scope: Met Slitter-1 & 2 |
|  | vkstech.com ¦ Free Industrial Knowledge for Packaging Professionals |  |

🎯 Purpose

To maintain uniformity of winding at slitters and avoid scratch defect on metallised finished rolls.

📊 Parameters — Width > 2500 mm on Unwinder

| Film | Speed (M/Min) | UW Tension | RW Tension | Nip Pressure |
| --- | --- | --- | --- | --- |
| 8 µ PET | 700 | Per recipe | Per recipe | Per recipe |
| 10 µ PET | 800 | Per recipe | Per recipe | Per recipe |
| 12 µ PET | 800 | Per recipe | Per recipe | Per recipe |
| 23 µ PET | 700 | Per recipe | Per recipe | Per recipe |

Tension and Pressure characteristic graphs are saved in the machine permanently for operator reference.

👤 Responsibility

Slitter Operators: Follow set points strictly per micron. Check nip roller surface before every run.

Supervisor: Verify finished rolls are scratch-free with visual inspection under proper lighting.

⚠️ Scratches on metallised film = customer rejection. Clean all rollers with IPA before every slitting run.