|  | VKS TECH Met Operational Excellence | Doc: VKS/MET/WI/01 Rev: 01 April 2026 |
| --- | --- | --- |
|  | Bare Film Selection for Metallizer | Scope: Met-1 & Met-2 |
|  | vkstech.com ¦ Free Industrial Knowledge for Packaging Professionals |  |

🎯 Purpose

Select the correct bare film roll for metallization as per production planning, ensuring correct metallization side, shield selection, and roll preparation.

👤 Responsibility

Metallizer Operator and Metallizer Supervisor.

📋 Procedure

Step 1 — Check Planning Format

Open Planning Format (MET/F/04). Identify which roll is scheduled for the current run.

Step 2 — Select Roll as Per Plan

Locate the correct roll in the storage area. Verify roll ID matches the planning sheet.

Step 3 — Check Metallization Side

Confirm which side of the film is to be metallized (corona treated side or plain side). Wrong side metallization = entire jumbo wasted.

Step 4 — Transport Roll

Bring the roll using overhead crane to the area behind the metallizer machine. Use proper sling belt and foam protection.

Step 5 — Select Shield Plate

Choose the suitable shield plate according to roll width. Shield must not touch the film edges — maintain tolerance limit distance.

Step 6 — Prepare Shields

After cleaning aluminium deposits from shields, apply graphite suspension paint. This protects shields from aluminium buildup and allows easy removal of deposits in the next cycle.

Step 7 — Shield Positioning

Take the shield up. Adjust the shield plate position so it does not touch the film ends. Maintain tolerance gap on both sides.

⚠️ Always verify metallization side BEFORE loading. Wrong side = full jumbo rejection. Check planning format twice.