|  | VKS TECH Met Operational Excellence | Doc: VKS/MET/WI/02 Rev: 01 April 2026 |
| --- | --- | --- |
|  | Boat Change Programme | Scope: Met-1 & Met-2 |
|  | vkstech.com ¦ Free Industrial Knowledge for Packaging Professionals |  |

🎯 Purpose

Standard procedure for ceramic evaporation boat changeover to ensure clean source section, proper boat installation, and contamination-free next production cycle.

📋 Procedure — Boat Changeover Checklist

A. Clean Evaporator Side Thoroughly

Remove all aluminium deposits from the source section using dedicated scraping tools. Use vacuum cleaner to collect all aluminium dust.

B. Clean Drum and Shield

Remove aluminium oxide deposits from the chill drum surface and all coating shields. Use drum cleaner tool + acetone for perfect cleaning.

C. Vacuum Clean Source Area

Use vacuum cleaner to remove ALL remaining aluminium dust from the entire source section. No dust particles should remain.

D. Follow Individual Roll Cycle Procedures

Complete all steps from the per-cycle maintenance checklist (WI-16) before installing new boats.

E. Install New Boats with Graphite Foil

Use graphite foil at both ends of each boat for proper electrical contact with copper clamps. This ensures uniform heating across the boat length.

F. Tighten Boats Properly

Boats must be fitted tightly in the copper clamps. Uneven tightening causes hot spots → premature boat cracking. Use even torque on both ends.

G. Clean All Rollers and Plasma

Wipe all guide rollers with IPA. Clean plasma treater unit. Ensure no contamination carries over to the new production cycle.

⚠️ A sloppy boat change = pinholes + OD problems for the entire next cycle. Take 15 extra minutes for a thorough changeover — it saves hours of troubleshooting later.