|  | VKS TECH Met Operational Excellence | Doc: VKS/MET/WI/04 Rev: 01 April 2026 |
| --- | --- | --- |
|  | Coating Drum Cleaning | Scope: Met-1 & Met-2 |
|  | vkstech.com ¦ Free Industrial Knowledge for Packaging Professionals |  |

🎯 Purpose

Clean the chill drum surface to remove all aluminium deposits, masking tape residue, and contaminants before loading the next production roll.

👤 Responsibility

Metallizer Operator and Trainee Operator.

📋 Procedure

Step 1 — Remove Film from Drum

Ensure all film is removed from the drum surface. No film remnants should remain.

Step 2 — Rotate Drum Using Foot Switch

Run the drum slowly using the foot switch. This allows cleaning the entire circumference while the drum rotates.

Step 3 — Clean with Drum Cleaner Tool

Use the dedicated drum cleaner tool to scrape off all aluminium deposits from the entire drum surface. Work systematically from one edge to the other.

Step 4 — Final Clean with Acetone

Apply acetone on a lint-free cloth and wipe the entire drum surface for a perfect finish. Ensure no residue remains.

Step 5 — Caustic Soda for Stubborn Deposits (if needed)

For stubborn deposits, use mild caustic soda solution (less than 20%). Apply carefully with cloth.

⚠️ MANDATORY: Use RUBBER hand gloves when using caustic soda. Caustic soda WILL BURN your hands if contact occurs. Wash with water immediately if skin contact happens.