|  | VKS TECH Met Operational Excellence | Doc: VKS/MET/WI/09 Rev: 01 April 2026 |
| --- | --- | --- |
|  | Metallizer Maintenance Work in Every Cycle | Scope: Met-1 & Met-2 |
|  | vkstech.com ¦ Free Industrial Knowledge for Packaging Professionals |  |

🎯 Purpose

Mandatory maintenance tasks to be performed between every boat cycle (changeover) to ensure consistent quality in the next production run.

📋 Per-Cycle Maintenance Checklist

A. Check and clean all ceramic boats. Remove any cracked or damaged boats.

B. Check and correct wire feed unit positioning. Verify wire alignment to boat center.

C. Clean the shutter mechanism. Ensure smooth open/close operation.

D. Clean dust particles from inside the entire chamber using vacuum cleaner.

E. Clean all shields and apply fresh release paint (graphite suspension/BN spray).

F. Clean the chill drum surface and apply new masking tape on edges.

G. Check shield settings and adjust positioning if required (gap uniformity both sides).

H. Load new bare roll on unwinder. Unload rewinder roll and lock properly.

I. Thread film through web path as per the customer's required metallization side (corona/plain).

J. Place proper core on the rewinder side (correct diameter, undamaged, clean).

⚠️ Skipping even ONE step from this checklist leads to defects in the next cycle. This 15-minute investment prevents hours of troubleshooting. Every item is mandatory — not optional.