|  | VKS TECH Met Operational Excellence | Doc: VKS/MET/WI/10 Rev: 01 April 2026 |
| --- | --- | --- |
|  | Cork Tape Layering on Slitter Rewinder Rollers | Scope: Met Slitter-1 & 2 |
|  | vkstech.com ¦ Free Industrial Knowledge for Packaging Professionals |  |

🎯 Purpose

Standard method of applying cork tape on slitter rewinder rollers to ensure optimum friction, uniformity, and longevity during PET film slitting operations. Applicable for BOPET, BOPP, and CPP films.

📐 Recommended Wrapping Angle

| Angle | Advantage | Recommendation |
| --- | --- | --- |
| 30° | Strongest grip, longest tape life, ideal for high-speed | Best for high-speed slitters |
| 45° | Easier to apply, good adhesion and smoothness | Good general purpose |
| >60° or 90° | Edges lift, vibration risk | NOT recommended |

📋 Step-by-Step Procedure

Step 1 — Surface Preparation

Clean the roller surface thoroughly with IPA or ethyl compound. Ensure it is dry, dust-free, and free from oil or residue.

Step 2 — Starting Point

Fix the first end of cork tape flat (0°) for 2 turns to anchor it properly. Press firmly to eliminate air bubbles.

Step 3 — Spiral Wrapping

Wrap the tape at 30°-45° angle uniformly along the roller length. Maintain firm, even tension — do not overstretch. Keep 2-3 mm overlap between turns (no gaps or excess overlap).

Step 4 — Finishing

End the wrapping with 2 flat turns at 0° to lock the tape. Secure the end using high-temperature adhesive tape or epoxy sealant.

Step 5 — Optional Heat Curing

If adhesive-backed tape is used, apply warm air at 80-100°C for a few minutes. Ensures better bonding and removes trapped air.

⚠️ Expected result: Smooth, balanced roller surface with strong friction on PET cores. No film slippage during slitting. Typical tape life: >6 months.