|  | VKS TECH Met Operational Excellence | Doc: VKS/MET/WI/14 Rev: 01 April 2026 |
| --- | --- | --- |
|  | AlOx Film Metallisation & Handling After Metallisation | Scope: Met-1 (AlOx Capable) |
|  | vkstech.com ¦ Free Industrial Knowledge for Packaging Professionals |  |

🎯 Purpose

AlOx (Aluminium Oxide) film is a specialty high-barrier product requiring utmost care during metallization and post-processing. This WI defines the complete process.

📋 Process Steps — Activity Wise

| # | Activity | Responsible |
| --- | --- | --- |
| 1 | Deep cleaning — remove all white dust from metalliser | Main Operator |
| 2 | Replace all boats with NEW boats | Main Operator |
| 3 | Clean all rollers with air and wet cloth | Asst. Operator |
| 4 | Clean and calibrate inline OD sensors | E&I Technician |
| 5 | Ensure O₂ cylinders are fully filled (150 bar) | Shift Engineer |
| 6 | Start first roll with normal OD 2.2 on new boats | Main Operator |
| 7 | Set up for AlOx: bypass DTR1 roller from web path | Main Operator |
| 8 | Select AlOx recipe. Stabilize Metal OD at 0.45 in AUTO mode | Main Operator |
| 9 | Start AlOx process. Manual correction for target OD within spec | Main Operator |
| 10 | Provide sample to QA Lab for barrier testing after 24 hours | Shift Engineer |

📊 Machine Parameters

| Parameter | Target | Tolerance |
| --- | --- | --- |
| Metal OD | 0.45 | UCL 0.47 / LCL 0.42 |
| AlOx Target OD | 0.11 | N/A |
| Base Film Transmittance | 88% | ±1% |

Frequency: Maximum 5 rolls of 26,000 m per boat cycle for AlOx.

Curing time: 40 days from manufacturing date before topcoat application.

🧤 Handling Rules After Metallisation

1. Never place rolls directly on the floor — always use sufficient cushion.

2. Store rolls hanging on end ply during storage.

3. Avoid touching the AlOx side during testing.

4. During slitting, path rollers must be covered with soft cork tape to prevent scratches.

⚠️ AlOx coating is less than 40nm thick — extremely delicate. Any mishandling destroys barrier properties permanently. Handle with extreme care.