|  | VKS TECH Met Operational Excellence | Doc: VKS/MET/WI/16 Rev: 01 April 2026 |
| --- | --- | --- |
|  | Slitting Process for Critical Customers | Scope: Met Slitter-1 & 2 |
|  | vkstech.com ¦ Free Industrial Knowledge for Packaging Professionals |  |

🎯 Purpose

Special handling procedures for critical customer orders (export customers, high-value brands) during slitting operations.

📋 Key Requirements

1. Critical customer material must ALWAYS be placed at CENTER position on the slitter — never at edge positions.

2. Direction arrow marking must be applied on all critical customer rolls (indicating metallization side orientation).

3. Extra quality inspection under proper lighting is mandatory before wrapping.

4. Joint count limits: Domestic = maximum 2 joints per roll. Export = maximum 1 joint per roll.

5. Masking tape must not extend more than 3 mm inside the film edge. Edge damage = downgrade = operator responsibility.

6. SAP Roll Availability must be verified BEFORE starting slitting. Wrong slitting without checking = penalty.

7. All critical customer rolls must be documented with additional remarks in the slitter logbook.

⚠️ Critical customer rejection impacts the entire company reputation. One downgraded roll to an export customer can lose a multi-crore annual contract. Treat every critical customer roll as if it is the only roll you will produce today.