|  | VKS TECH Met Operational Excellence | Doc: VKS/MET_SL/WI/04 Rev: 01 April 2026 |
| --- | --- | --- |
|  | Receiving and Inspecting Paper Cores | Scope: Met Slitter-1 & 2 |
|  | vkstech.com ¦ Industrial Knowledge for Packaging Professionals |  |

🎯 Purpose

Inspect paper cores before slitter use. Damaged or incorrect cores cause telescoping, starring, and winding defects that downgrade finished rolls.

👤 Responsibility

Slitter Operator (inspection). Supervisor (rejection authority).

📋 Procedure

Step 1 - Receive from Store

Collect cores with requisition slip. Verify quantity matches.

Step 2 - Visual Inspection

Inspect EACH core for: dents or crushing (from handling), delamination of paper layers, moisture damage (soft/swollen areas), ovality (not perfectly round).

Step 3 - Verify Core ID

Measure internal diameter: 3 inch (76.2mm), 6 inch (152.4mm), or 8 inch (203.2mm) per slitting plan. Wrong core ID = roll will not fit on customer unwinder.

Step 4 - Verify Wall Thickness

Check wall thickness: 12/13/14/15/16/17/19mm as specified. Wrong thickness affects unwinder stop diameter at customer machine.

Step 5 - Check Core Type

Verify Recycled (RC) or New - use exactly as planned. Some customers mandate new cores for export.

Step 6 - Stack Accepted Cores

Stack vertically in designated area near slitter, separated by size.

Step 7 - Reject Damaged

Any defective core goes to rejection area immediately. Never mix with accepted cores.

A damaged core looks fine until wound. Then it creates telescoping and starring. 30 seconds of inspection prevents a Rs.10,000+ rejection.