|  | VKS TECH Met Operational Excellence | Doc: VKS/MET_SL/WI/06 Rev: 01 April 2026 |
| --- | --- | --- |
|  | Slitting Start - Running and Quality Monitoring | Scope: Met Slitter-1 & 2 |
|  | vkstech.com ¦ Industrial Knowledge for Packaging Professionals |  |

🎯 Purpose

Standard procedure for starting slitting and continuous quality monitoring during production.

👤 Responsibility

Supervisor (monitoring). Operator (execution). QC Officer (post-slitting).

📋 Procedure

Step 1 - Final Verification

Confirm all setup complete: widths measured, blades aligned, cores fixed, film threaded, tension set. Only then press START.

Step 2 - Continuous Monitoring

Supervisor MUST visually monitor ALL rolls while running. Walk the rewinder length. Look at each roll. This is NOT optional.

Step 3 - Watch for Defects

During run watch for: rough cutting edges, wrinkles, ripple marks, edge curl, telescoping forming, unusual sounds from blade or roller contact.

Step 4 - Post-Slitting QC

ALL rolls inspected by QC Officer under proper lighting. Check: OD consistency, scratch marks, crease, edge quality, joint tagging.

Step 5 - Grade Each Roll

Enter grade per roll in slitting register:

| Grade | Meaning | Action |
| --- | --- | --- |
| 2 | OK - meets all specs | Wrap and dispatch |
| 3 | Downgraded / B-Grade | Separate + document reason |
| 5 | Salvageable | Re-slit if possible |
| 6 | Offcut / Waste | Bag separately by shift |
| 7 | To Coating Dept | Transfer with docs |
| 8 | OK but order awaited | Store in holding area |

One unwatched defect at 800 m/min = hundreds of metres waste. Continuous monitoring = the difference between 2% waste and 0.5% waste.